Policarbonato - P.C.

Chemical	Polycarbonate

Designation:

DIN Abbreviation:	PC

Colour, Filler:	Transparent

Stock Availability:	Standard length 3 metres, also cut to size

¯ Rod 	4  -   250 mm dia

¯ Plate	1  -   100 mm thick

¯ Tube	up to 200 mm OD

¯ Profile

¯ Finished parts, machined or injection moulded

Policarbonato P;C.  is an amorphous engineering thermoplastic with high transparency and toughness for varied applications.

Main characteristics:	¯ transparent	¯ easily machined and polished,

¯ very tough	  care required with coolant,

¯ strong	  susceptible to stress cracking

¯ good heat deformation		¯ easily welded

resistance	 	¯ easily bonded

¯ good electrical insulation

Preferred Fields:	Mechanical engineering, model making, automotive engineering, transport and conveyor technology, electrical engineering, precision engineering, household appliances, food technology, medical technology, photo technology, buildings

Applications:	¯ transparent working models	¯ housing parts

¯ insulators		¯ plugs

¯ plug strips		¯ sight glasses

¯ masking covers		¯ optical components

¯ photo couplers		¯ weather protection parts

Policarbonato - P.C.

The following information corresponds with our current knowledge and indicates our products and possible applications. We cannot give a legally binding guarantee of certain properties or the suitability for a specific application. Existing commercial patents must be observed. A definitive quality guarantee is given in our general conditions of sales. Unless otherwise stated, these values represent averages taken from injection moulding samples. We reserve the right of technical alterations.

| Properties | Unit | Test method DIN ASTM |  |
| --- | --- | --- | --- |
| Mechanical |  |  |  |
| Density | g/cm³ | 53 479 | 1.20 |
| Tensile strength at yield | MPa | 53 455 | 65 |
| Tensile strength at break | MPa | 53 455 |  |
| Elongation at break | % | 53 455 | 60 - 100 |
| Modulus of elasticity in tension | MPa | 53 457 | 2200 |
| Modulus of elasticity in flexure | MPa | 53 457 |  |
| Ball indentation hardness | MPa | 53 456 | 100 |
| Impact strength (Charpy) | kJ/m2 | 53 453 | no br. |
| Creep rupture strength after 1000 hrs with static load | MPa |  | 48 |
| Time yield limit for 1% elongation after 1000 hrs. | MPa |  | 18 |
| Coefficient of friction against hardened and ground steel p = 0,05 N/mm², v = 0,6 m/s | – |  | 0.52 - 0.58 |
| Wear conditions as above | µm/km |  | 22 |
| Thermal |  |  |  |
| Crystalline melting point | °C | 53 736 |  |
| Glass transition temperature | °C | 53 736 | 145 |
| Heat distortion temperature Method A Method B | °C °C | ISO 75 ISO 75 | 135 140 |

| Properties | Unit | Test method DIN ASTM |  |
| --- | --- | --- | --- |
| Thermal |  |  |  |
| Max. service temperature short term long term | °C °C |  | 140 120 |
| Coefficient of thermal conductivity | W/(m . K) |  | 0.19 |
| Specific heat | J/(g . K) |  | 1.2 |
| Coefficient of thermal expansion | 10-5/K |  | 6 - 7 |
| Electrical |  |  |  |
| Dielectric constant at 105 Hz |  | 53 483 | 3 |
| Dielectric loss factor at 105 Hz |  | 53 483 | 0.006 |
| Specific volume resistance | W . cm | 53 482 | 1017 |
| Surface resistance | W | 53 482 | 1015 |
| Dielectric strength 1 mm | kV/mm | 53 481 | 27 |
| Tracking resistance |  | 53 480 | KA 1 |
| Miscellaneous |  |  |  |
| Moisture absorption: Equilibrium in standard atmosphere (23 °C / 50 % relative humidity) | % | 53 714 | 0.2 |
| Water absorption at saturation at 23 °C | % | 53 495 | 0.36 |
| Resistance to hot water, washing soda |  |  | not resistant |
| Flammability |  | UL 94 | V2 |
| Resistance to weathering |  |  | not resistant |

* after storage in a standard 23/50 atmosphere (DIN 50 014) to equilibrium