P.E.E.K. mod.

Chemical	Polyetheretherketone

Designation:

DIN Abbreviation:	PEEK

Colour, Filler:	black

10% carbon, graphite, PTFE

Stock Availability:	Standard lengths 3 metres, also cut to size

¯ Rod 	4  -   100 mm dia

¯ Plate	5  -     50 mm thick

¯ Tube	up to 150 mm OD

¯ Pressed discs, rings, bushes

¯ Profile

¯ Finished parts, machined or injection moulded

P.E.E.K. mod. is a semicrystalline high performance thermoplastic with optimized tribological properties for demanding bearing and friction requirement.

Main characteristics:	¯ very good sliding properties	¯ high wear resistance

even without lubrication	¯ very rigid

¯ high thermal mechanical	¯ high creep strength

bearing strength	¯ not electrically insulating

¯ good chemical resistance	¯ good machinability

¯ hydrolysis resistant, even	¯ resistance to gamma radiation

against superheated steam

Preferred Fields:	Mechanical and automotive engineering, nuclear and vacuum

technology, transport and conveyor technology, textile, packaging

and paper processing machinery, precision and chemical engineering, 	aircraft and aerospace industry, plant construction.

Applications:	¯ friction bearings		¯ wear strips

¯ static/dynamic high bearing	¯ gears

strength parts		¯ thrust washers

¯ slide shoes		¯ ball valve seals

¯ chain bearings		¯ slide rings

¯ sealing rings		¯ piston rings

P.E.E.K. mod.

The following information corresponds with our current knowledge and indicates our products and possible applications. We cannot give a legally binding guarantee of certain properties or the suitability for a specific application. Existing commercial patents must be observed. A definitive quality guarantee is given in our general conditions of sales. Unless otherwise stated, these values represent averages taken from injection moulding samples. We reserve the right of technical alterations.

| Properties | Unit | Test method DIN ASTM |  |
| --- | --- | --- | --- |
| Mechanical |  |  |  |
| Density | g/cm³ | 53 479 | 1.48 |
| Tensile strength at yield | MPa | 53 455 |  |
| Tensile strength at break | MPa | 53 455 | 118 |
| Elongation at break | % | 53 455 | 3 |
| Modulus of elasticity in tension | MPa | 53 457 | 10000 |
| Modulus of elasticity in flexure | MPa | 53 457 | 8100 |
| Ball indentation hardness | MPa | 53 456 |  |
| Impact strength (Charpy) | kJ/m² | 53 453 |  |
| Creep rupture strength after 1000 hrs with static load | MPa |  |  |
| Time yield limit for 1% elongation after 1000 hrs. | MPa |  |  |
| Coefficient of friction against hardened and ground steel p = 0,05 N/mm², v = 0,6 m/s | – |  | 0.11 |
| Wear conditions as above | µm/km |  |  |
| Thermal |  |  |  |
| Crystalline melting point | °C | 53 736 | 334 |
| Glass transition temperature | °C | 53 36 | 143 |
| Heat distortion temperature Method A Method B | °C °C | ISO 75 ISO 75 | 277 |

| Properties | Unit | Test method DIN ASTM |  |
| --- | --- | --- | --- |
| Thermal |  |  |  |
| Max. service temperature short term long term | °C °C |  | 300 250 |
| Coefficient of thermal conductivity | W/(m . K) |  | 0.24 |
| Specific heat | J/(g . K) |  |  |
| Coefficient of thermal expansion | 10-5/K |  |  |
| Electrical |  |  |  |
| Dielectric constant at 105 Hz |  | 53 483 |  |
| Dielectric loss factor at 105 Hz |  | 53 483 |  |
| Specific volume resistance | W . cm | 53 482 |  |
| Surface resistance | W | 53 482 |  |
| Dielectric strength at 1 mm | kV/mm | 53 481 |  |
| Trecking resistance |  | 53 480 |  |
| Miscellaneous |  |  |  |
| Moisture absorption: Equilibrium in standard atmosphere (23 °C / 50 % rel. humidity) | % | 53 714 |  |
| Water absorption at saturation at 23 °C | % | 53 495 | 0.1 |
| Resistance to hot water, washing soda |  |  | resistant |
| Flammability |  | UL 94 | VO |
| Resistance to weathering |  |  | resistant |

after storage in a standard 23/50 atmosphere (DIN 50 014) to equilibrium